## Slide 1
A Detailed Mathematical Model for Evaluation of Solid Oxide Fuel Cells Performance Degradation
Mina Naeini (PhD candidate McMaster university)
Dr. J. Cotton, Dr. T. Adams

## Slide 2
Performance degradation
)
Parhizkar, T., & Roshandel, R. (2017). Long term performance degradation analysis and optimization of anode supported solid oxide fuel cell stacks. Energy conversion and management, 133, 20-30.
= Open-Circuit voltage
= Ohmic polarization
= Concentration polarization
= Activation polarization

## Slide 3
1
2
3
1
Performance degradation, makes it hard to find the proper sizing and operation of SOFCs for the communities.
2
Lack of a comprehensive model that accounts for the dominant degradation mechanisms in SOFCs prevents widespread commercialization of this technology.
3
Resolve the apparent conflict in the literature about whether temperature positively or negatively correlates to the SOFCs performance degradation.

## Slide 4
M. Naeini, J.S. Cotton, T.A. Adams II, A mathematical model for prediction of long-term degradation effects in solid oxide fuel cells, J. Power Sources, Under review.

## Slide 5: Thermodynamic equations
()
Current
Electrical conductivity
Length
Area
Temperature
Electrons associated with a reaction
Partial pressure of species i
Operating current density
Exchange current density

## Slide 6: System degradation mechanisms
Pore diameter
Particle size of species i
= Volume fraction of species i

## Slide 7: System degradation mechanisms Sulfur poisoning of hydrocarbon-fueled SOFCs
Previous models focused on performance loss in H2-fueled SOFCs.
H2S deactivates catalytic activity of SOFCs by reducing electrochemical activity and hydrocarbon conversion.
The models developed for H2-fueled SOFCs cannot be used for hydrocarbon-fueled ones.

## Slide 8: System degradation mechanisms Sulfur poisoning of hydrocarbon-fueled SOFCs
Experimental data from: A. Hagen, G.B. Johnson, P. Hjalmarsson, Electrochemical evaluation of sulfur poisoning in a methane-fuelled solid oxide fuel cell: Effect of current density and sulfur concentration, J. Power Sources. 272 (2014) 776–785.
and = Weighting factors

## Slide 9
Validation of the model
Chart: Time (h)
| 0 | 200 | 400 | 600 | 800 | 1000 | 1200 | 1400
Experimental Data | 0.62792 | 0.60195 | 0.57987 | 0.55649 | 0.54351 | 0.53182 | 0.52273 | 0.51623
Model | 0.62676 | 0.59234 | 0.56512 | 0.54466 | 0.52992 | 0.51971 | 0.51291 | 0.50862
Experimental data from: A. Hagen, R. Barfod, P.V. Hendriksen, Y.L. Liu, S. Ramousse, Degradation of anode supported SOFCs as a function of temperature and current load, J. Electrochem. Soc. 153 (2006) 1165–1171.
Voltage profile over time for the SOFC running at 750℃ and 0.75 A/cm2

## Slide 10
Voltage loss and degradation rate
Chart: Time (h)
| 1 | 120 | 240 | 360 | 480 | 600 | 720 | 840 | 960 | 1080 | 1200 | 1320 | 1440 | 1560 | 1680 | 1800 | 1920 | 2040 | 2160 | 2280 | 2400 | 2520 | 2640 | 2760 | 2880 | 3000 | 3120 | 3240 | 3360 | 3480 | 3600 | 3720 | 3840 | 3960 | 4080 | 4200 | 4320 | 4440 | 4560 | 4680 | 4800 | 4920 | 5040 | 5160 | 5280 | 5400 | 5520 | 5640 | 5760 | 5880 | 6000
V | 0.76537 | 0.75292 | 0.74192 | 0.73237 | 0.72423 | 0.71738 | 0.71167 | 0.70695 | 0.70308 | 0.69992 | 0.69733 | 0.69521 | 0.6921 | 0.68984 | 0.68774 | 0.68579 | 0.68397 | 0.68225 | 0.68064 | 0.67911 | 0.67766 | 0.67628 | 0.67496 | 0.6737 | 0.6725 | 0.67134 | 0.67023 | 0.66917 | 0.66814 | 0.66714 | 0.66618 | 0.66526 | 0.66436 | 0.66349 | 0.66264 | 0.66182 | 0.66103 | 0.66025 | 0.6595 | 0.65876 | 0.65804 | 0.65735 | 0.65666 | 0.656 | 0.65535 | 0.65471 | 0.65409 | 0.65348 | 0.65289 | 0.6523 | 0.65173
rd | 14.3024 | 12.9838 | 11.5281 | 10.0382 | 8.5968 | 7.2615 | 6.0664 | 5.026 | 4.1403 | 3.4599 | 3.0445 | 2.7433 | 2.5 | 2.33 | 2.2014 | 2.0725 | 2.0004 | 1.9224 | 1.8413 | 1.7863 | 1.7006 | 1.6229 | 1.5521 | 1.4874 | 1.4279 | 1.3732 | 1.3225 | 1.2755 | 1.2319 | 1.1911 | 1.1531 | 1.1174 | 1.0839 | 1.0524 | 1.0228 | 0.99476 | 0.96828 | 0.9432 | 0.91941 | 0.89682 | 0.87534 | 0.85488 | 0.83538 | 0.81677 | 0.79899 | 0.78198 | 0.76569 | 0.75009 | 0.73512 | 0.72075 | 0.70706
Voltage profile over time, and Degradation rate percentage per 1000 hours versus time for the SOFC running at 750℃ and 0.5 A/cm2, with pure hydrogen.

## Slide 11
Sensitivity analysis
Generate 6000 random operating conditions
Current density (0.2-1 A/cm2), Temperature (873-1173 K), H2 partial pressure (70%-90% of the fuel pressure)
Simulate 3000 hours of operation of SOFCs at each condition
Calculate average degradation rates over the first, second, and third 1000 hours of operation for each random sample

## Slide 12
Sensitivity analysis

## Slide 13: Conclusion
The first complete model of long-term SOFCs performance degradation
Combined information from the literature with very little parameter fitting
Validated on literature data not used to develop the model

## Slide 14
THANK YOU