Supplementary material for: Physics-Consistent Hybrid Deep Learning for Daily Energy Prediction and Multi-Objective Energy–CO₂–Cost Optimization in Aluminium Cold Rolling

Hyeonrok Choia,b, Jiseon Parka , Won Yanga and Seong-il Kima,c*

a Low-Carbon Emission Control R&D Department, Research Institute of Sustainable Development Technology, Korea Institute of Industrial Technology, Cheonan 31056, Republic of Korea

b School of Mechanical Engineering, Sungkyunkwan University, Suwon 16419, Republic of Korea

c Green Process and Energy System Engineering, University of Science and Technology, Cheonan, Chungnam, Republic of Korea

* Corresponding Author: ksungil85l@kitech.re.kr.

Supplementary Table S1. Description

Supplementary Table S1 summarises the statistical characteristics of the aluminium cold rolling database used to develop the daily energy consumption model. For each rolling mill (RM4–RM6), the table reports the minimum, maximum, average, and standard deviation of daily production, pass-wise reduction ratio, tension, and rolling speed, as well as exit thickness for each pass. These statistics characterise the typical operating window and variability of the three mills and indicate that the data cover a wide range of production levels and operating conditions while maintaining tight control of final strip thickness. The ranges reported in Table S1 were used to define realistic bounds and constraints for model training and for the subsequent multi-objective optimisation.

Supplementary Table S2. Description

Supplementary Table S2 summarises the analytical rolling-energy model used in this study. For each physical quantity, the table lists the parameter name, description, governing equation, symbol, and literature source. The model starts from the mean rolling pressure and mean tension, then defines mean yield shear stress and mean yield stress based on the Ludwik work-hardening law. Using these quantities, cumulative strain, flow stress, rolling force, and the flattened roll radius are computed, followed by torque, mechanical power, and per-pass energy consumption. The definitions of geometric and operating variables (e.g. mean thickness, strip width, contact length, roll radius, arm coefficient, mechanical efficiency) are also provided. These relationships form the physics-based core of the rolling-energy module that is coupled with the data-driven network in the hybrid surrogate model.

Supplementary Table S3. Description

Supplementary Table S3 lists the CO₂ emission factors and usage ratios used to quantify daily emissions from the aluminium cold rolling process. For each component, the table reports the parameter symbol, description, unit, and numerical value. The CO₂ emission factors include grid electricity (αelect,ton CO₂-eq/MWh, primary aluminium production (αraw​, ton CO₂-eq/ton Al), rolling lubricant (αlub​, ton CO₂-eq/ton Al), and chemical additives (αadd​, ton CO₂-eq/ton Al). In addition, lubricant and additive usage ratios (rlubr​, ton/ton Al) are provided to convert daily aluminium throughput into corresponding lubricant and additive consumption. These parameters are used in the main text to compute total daily CO₂ emissions as the sum of contributions from electricity use, primary aluminium input, lubricant, and additives.

Supplementary Table S4. Description

Supplementary Table S4 lists the economic and cost-related parameters used in the aluminium cold rolling analysis. For each parameter, the table reports the description, unit, and numerical value. The parameters include the average electricity price pelect​ (USD/MWh), ETS carbon price pETS(USD/ton CO₂), raw material cost craw​ (USD/ton Al), capital cost per cold rolling line Cinv​ (USD), O&M cost rate rO&M(% of CAPEX), and the number of operating days per year Nop(day/year). These values are used in the main text to compute daily operating cost and specific production cost (SPC) in the multi-objective optimisation.

Table S1. Statistical summary of the aluminium cold rolling database used for energy consumption modelling.

|  |  |  |  | Min |  |  |  | Max |  |  |  | Average |  |  | Standard deviation |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | RM4 | RM5 | RM6 | RM4 |  | RM5 | RM6 | RM4 |  | RM5 | RM6 |  | RM4 | RM5 | RM6 |
| Production (ton) |  |  |  | 7.88 | 2.10 | 5.02 | 221.9 |  | 278.2 | 159.7 | 104.9 |  | 88.08 | 46.15 |  | 40.33 | 64.67 | 27.71 |
| Reduction (%) | Pass 1 |  |  | 35.50 | 34.50 | 34.00 | 41.20 |  | 40.50 | 40.00 | 39.04 |  | 38.64 | 38.17 |  | 1.36 | 1.30 | 1.25 |
|  | Pass 2 |  |  | 35.00 | 34.50 | 34.00 | 40.50 |  | 39.80 | 39.20 | 38.49 |  | 38.10 | 37.61 |  | 1.35 | 1.22 | 1.19 |
|  | Pass 3 |  |  | 30.14 | 30.37 | 29.93 | 35.00 |  | 35.00 | 35.00 | 34.16 |  | 34.21 | 34.19 |  | 1.00 | 0.95 | 0.90 |
|  | Pass 4 |  |  | 27.03 | 26.45 | 26.01 | 35.00 |  | 35.00 | 35.00 | 31.49 |  | 31.81 | 32.04 |  | 1.49 | 1.46 | 1.38 |
|  | Pass 5 |  |  | 23.60 | 21.45 | 20.64 | 33.70 |  | 35.00 | 34.90 | 28.90 |  | 29.37 | 29.88 |  | 1.69 | 1.64 | 1.65 |
|  | Pass 6 |  |  | 5.93 | 6.12 | 5.92 | 30.00 |  | 29.88 | 30.00 | 20.01 |  | 21.13 | 22.32 |  | 5.34 | 5.20 | 4.79 |
| Tension (kN) | Pass 1 |  |  | 33.94 | 27.93 | 29.97 | 68.34 |  | 63.81 | 63.25 | 49.92 |  | 47.21 | 49.33 |  | 5.85 | 5.64 | 5.77 |
|  | Pass 2 |  |  | 41.05 | 39.28 | 40.99 | 74.37 |  | 72.25 | 73.20 | 58.40 |  | 55.60 | 57.74 |  | 5.67 | 5.52 | 5.30 |
|  | Pass 3 |  |  | 54.97 | 52.97 | 56.67 | 82.08 |  | 79.26 | 83.65 | 69.88 |  | 68.41 | 71.71 |  | 4.31 | 4.53 | 4.62 |
|  | Pass 4 |  |  | 54.79 | 51.42 | 55.05 | 86.75 |  | 85.40 | 91.61 | 71.11 |  | 70.40 | 74.43 |  | 5.03 | 5.00 | 5.21 |
|  | Pass 5 |  |  | 60.34 | 57.84 | 59.02 | 95.62 |  | 98.28 | 98.11 | 78.03 |  | 77.39 | 82.08 |  | 5.17 | 5.07 | 5.46 |
|  | Pass 6 |  |  | 35.81 | 33.01 | 34.35 | 93.46 |  | 92.36 | 96.52 | 67.99 |  | 68.48 | 74.33 |  | 11.38 | 11.23 | 10.63 |
| Speed (m/s) | Pass 1 |  |  | 8.33 | 8.33 | 8.33 | 12.07 |  | 11.77 | 12.20 | 9.67 |  | 9.46 | 10.32 |  | 0.79 | 0.73 | 0.81 |
|  | Pass 2 |  |  | 9.26 | 9.12 | 9.33 | 14.28 |  | 14.10 | 14.71 | 11.60 |  | 11.37 | 12.24 |  | 0.93 | 0.87 | 0.92 |
|  | Pass 3 |  |  | 9.50 | 9.23 | 10.73 | 16.31 |  | 15.57 | 16.60 | 12.98 |  | 12.76 | 13.64 |  | 1.06 | 1.00 | 1.03 |
|  | Pass 4 |  |  | 11.00 | 10.53 | 11.40 | 17.94 |  | 17.62 | 18.37 | 14.73 |  | 14.50 | 15.36 |  | 1.14 | 1.13 | 1.16 |
|  | Pass 5 |  |  | 12.93 | 13.39 | 13.32 | 20.13 |  | 20.04 | 20.53 | 16.76 |  | 16.58 | 17.31 |  | 1.24 | 1.19 | 1.24 |
|  | Pass 6 |  |  | 15.33 | 14.61 | 15.99 | 22.52 |  | 22.00 | 23.00 | 19.18 |  | 19.02 | 19.80 |  | 1.32 | 1.33 | 1.26 |
| Thickness (mm) | Exit 1 |  |  | 0.16 | 0.16 | 0.17 | 0.253 |  | 0.253 | 0.253 | 0.209 |  | 0.19 | 0.20 |  | 0.011 | 0.012 | 0.012 |
|  | Exit 2 |  |  | 0.10 | 0.10 | 0.10 | 0.154 |  | 0.154 | 0.165 | 0.132 |  | 0.12 | 0.12 |  | 0.007 | 0.0070 | 0.007 |
|  | Exit 3 |  |  | 0.06 | 0.06 | 0.07 | 0.099 |  | 0.099 | 0.11 | 0.088 |  | 0.08 | 0.08 |  | 0.004 | 0.005 | 0.004 |
|  | Exit 4 |  |  | 0.04 | 0.05 | 0.05 | 0.066 |  | 0.077 | 0.077 | 0.055 |  | 0.05 | 0.06 |  | 0.003 | 0.003 | 0.003 |
|  | Exit 5 |  |  | 0.03 | 0.03 | 0.03 | 0.044 |  | 0.055 | 0.066 | 0.044 |  | 0.04 | 0.04 |  | 0.002 | 0.002 | 0.003 |
|  | Exit 6 |  |  | 0.03 | 0.03 | 0.03 | 0.033 |  | 0.033 | 0.033 | 0.033 |  | 0.03 | 0.03 |  | 0.003 | 0.002 | 0.001 |

Table S2. Analytical rolling-energy model summary

| Parameter | Description | Equation | Symbol | Reference |
| --- | --- | --- | --- | --- |
| pm,p | Mean rolling pressure | pm= 2k(1-tm2k)hmμld(eμldhm-1) | hm: mean thickness (m), μ: fricition coefficieent, ld​ strip-roller contact length(m) | [1] |
| tm | Mean tension | tm= tb+tf2 | tb,tf: back/front tension | [1] |
| k | Mean yield shear stress | 2k=1,155Y | Y : mean yield stress (MPa) | [2] |
| Y | Mean yield stress | Y= 1εε0εtKεndε= K(εtn+1-ε0n+1)(εt-ε0)(n+1) | K: Ludwik coefficient (MPa) n: strain hardening exponent(-) εt, ε0: strains, (-) | [2] |
| εt | Cumulative strain | εt=ε0+∆ε | ∆ε : per-pass strain increment (-) | - |
| σ | Flow stress | σ= K εn | - | [3] |
| Fm,p | Rolling force | Fm,p= pmB∆hm,pR'm,p | B : strip width (m) ∆hm,p=hm,in-hm,out R'm,p: flattened radius (m) | [2] |
| R'm,p | flattened radius (m) | R'm,p=R(1+2.11×10-5(FB(hin-out)) | R: roll radius (m) | [3] |
| M | torque | M=2Fψld | ψ : arm coefficient | ψ=0.4 [4] |
| Wm,p | Power | Pm,p=Mωm,p=Mvm,pR'm,p | ωm,p: angular speed (rad/s) | [5] |
| Em,p | Energy consumption | Em,p= Wm,ptm,pη | tm,p: Process time (s) η: Mechanical efficiency(-) | [5] |

Table S3. CO2 emission factor for cold rolling process

| Component | Parameter | Description | Unit | Value |
| --- | --- | --- | --- | --- |
| CO2 emission facor | αelect | Grid electricity emission | ton CO2,eq/MWh | 0.4434 |
|  | αraw | primary aluminium emission | ton CO2,eq/ tonAl | 17.1 |
|  | αlub | Rolling lubricant emission | ton CO2,eq/ tonAl | 3.5 |
|  | αadd | Additive emission | ton CO2,eq/ tonAl | 8 |
| Usage ratio | rlub | Lubricant usage ratio | tonlub/tonAl | 0.071 |
|  | radd | Additive usage ratio | tonadd./tonAl | 0.062 |

Table S4. Economic and cost related parameters for aluminium cold rolling analysis

| Parameter | Description | Unit | Value |
| --- | --- | --- | --- |
| pelect | Average electricity price | $/MWh | 140 |
| pets | ETS carbon price | $/ tonCO2 | 6.61 |
| craw | Raw material cost | $/tonAl | 2370 |
| Cinv | Capital cost per cold rolling line | $ | 60 ×106 |
| rO&M | O&M cost rate | % | 5 |
| Nop | Operating day per year | Day/year | 330 |

References

Stone M. Rolling of thin strip. Iron Steel Eng 1953;2:61.

Poursina M, Dehkordi NT, Fattahi A, Mirmohammadi H. Application of genetic algorithms to optimization of rolling schedules based on damage mechanics. Simul Model Pract Theory 2012;22:61–73.

Farhatnia F, Salimi M. Effect of entry bending moment on exit curvature in asymmetrical rolling. Int J Eng Sci Technol 2011;3:0.

Babajamali Z, Khabaz MK, Aghadavoudi F, Farhatnia F, Eftekhari SA, et al. Pareto multi-objective optimization of tandem cold rolling settings for reductions and inter stand tensions using NSGA-II. ISA Trans 2022;130:399–408. 〈https://www.sciencedirect.com/science/article/pii/S0019057822001574〉.

Guo, Q., Zhou, Z., Li, J., & Jing, F. (2025). Mechanism- and data-driven algorithms of electrical energy consumption accounting and prediction for medium and heavy plate rolling. Electronic Research Archive, 33(1), 381–408. https://doi.org/10.3934/era.2025019.

© by the authors. Licensed to PSEcommunity.org and PSE Press. This is an open access article under the creative commons CC-BY-SA licensing terms. Credit must be given to creator and adaptations must be shared under the same terms. See https://creativecommons.org/licenses/by-sa/4.0/